FPE 2203 Physical Processing of Wood (3 CU)

# Course Name: PHYSICAL PROCESSING OF WOOD

# Course Code: FPE 2204

# Credit Units: 3 CU

# Contact Hours: 45

# Course Description

# The course introduces students to wood as an industrial raw material, and the various machinery, processes and methods required producing good quality timber.

Course Objectives

- To equip students with knowledge required for efficient conversion of logs into solid timber products in industry.

- To provide knowledge to students on appropriate post conversion processes, handling and storage of timber to ensure quality.

# Learning Outcomes

- The students should be able to make appropriate choices of machinery for specific wood raw material and intended quality of product in saw milling industry.

- Students should be able to apply the principles of timber seasoning and storage in managing saw mills.

Course Outline

- Introduction to wood processing; broad classification of forest products (2 LH)

- Wood as an industrial raw material (2 LH, 2 PH)

- Wood Machining: Orthogonal cutting and peripheral milling; Geometry of the saw tooth (4 LH, 4 PH)

- Tool-wood interactions during machining: Machining defects (3 LH, 4 PH)

- Sawmilling: Sawing methods and procedures; Machinery and plant layout; Sawn wood dimensions (4 LH, 6 LH)

- Factors affecting mill recovery (2 LH)

- Mill modernization and innovations (3 LH, 4 PH)

- Integration within the physical processing industries (4 LH)

- Timber seasoning: Objectives timber drying; Factors influencing timber drying; Drying methods (4 LH 6 PH)

- Timber grading (2 LH, 4PH)

# Mode of assessment

- Continuous assessment (coursework, test) = 40%

- University examinations = 60%

Basic Reading List

Ed M. Williston. (1988)Lumber manufacturing: The design and operation of sawmills and planer mills. Backbeat books. ISBN-13: 978-0879301743.

Jerome E. Carter (2006). Wood Utilization. Nova Science Publishers Inc. 978-1600214592

Kollman  F. P. and Cote W. A., jr (1968). Principles of Wood Science and Technology

M. A. Fonseca (2006). The Measurement of Roundwood: Methodologies and Conversion Ratios. CABI. 978-0851990798

Seerey, D.F. (2009). Small Sawmills : Their Equipment, Construction, and Operation. BiblioBazaar. ISBN: 978-1113897657.

United States Forest Service (2009). Rules and Regulations for the Grading of Lumber. BiblioBazaar. 978-1103219322.

William H. Brown (1989).The Conversion and Seasoning of Wood: A Guide to Principles and Practice. Linden Publishing. 978-0941936149.

Williston E. M., (1989). Saws: Design, Selection, Operation and maintenance.  Miller Freeman Publications, San Francisco